## Slide 1: TRAINING PROGRAMME FOR INDUSTRIAL ENTERPRISEs
Module 7.5:
Introducing characteristics of the technological line in the brick and ceramic manufacturing industry.
Technical staffs

## Slide 2: Content
INFORMATION ON TYPICAL TECHNOLOGICAL LINE CHARACTERISTICS
SOME TECHNOLOGICAL LINE CHARACTERISTICS IN BRICK AND CERAMIC PRODUCTION LINE

## Slide 3
INFORMATION ON TYPICAL TECHNOLOGICAL LINE CHARACTERISTICS
Brick and ceramic industry is one of the traditional construction materials industries in Vietnam. Contributing greatly to civil and industrial construction.
There are many brick and ceramic facilities in Vietnam and most of which are small and medium enterprises.
Large enterprises: Viglacera, Dong Tam, Prime Group, TTC, Mikado ...
Depending on the type of product, the Brick and ceramic industry can be divided into the following types
Enterprises producing Folk ceramics and fine arts
Enterprises producing construction ceramics
Enterprises producing Industrial ceramics
Enterprises producing fired bricks for construction
Enterprises producing concrete block for construction
Enterprises producing Aerated Autoclave Concrete (AAC)

## Slide 4: CERAMICS INDUSTRY
Introduction:
The Vietnamese ceramic industry has a long history, making important contributions to the country's culture and economy.
The diversity of ceramic types reflects the richness of art and application.
In addition to civil ceramic types, construction ceramic types and technical ceramic types are also strongly developed.

## Slide 5: CERAMICS INDUSTRY
History:
Vietnamese ceramics appeared in the Neolithic period, developing strongly through the Ly, Tran, and Le dynasties.
Ly - Tran period: Forming ceramic glaze lines such as jade glaze, white glaze, brown glaze, green glaze, brown flower and blue flower glaze.
Modern period: Combining traditional techniques and new technology, expanding export markets.
Current ceramic production situation:
Vietnam has about 2,000 traditional craft villages, including many famous ceramic production villages such as Bat Trang, Chu Dau, Phu Lang.
Vietnamese ceramic products are exported to many large markets such as the US, Japan, and the EU, with an export turnover of 711 million USD in 2022.
However, the largest ceramic production center in Vietnam today is Binh Duong province, with ceramic production accounting for 70% of the output of household ceramics.

## Slide 6: CERAMICS INDUSTRY
Chart: Vietnam's ceramic exports in the period 2019 - 2023
| Năm 2019 | Năm 2020 | Năm 2021 | Năm 2022 | Năm 2023
Cột1
Kim ngạch(triệu USD) | 539.1 | 581 | 674.7 | 710.7 | 618.5
Tăng trưởng(%) | 5.9 | 7.8 | 16.1 | 5.3 | -13
Turnover (Million USD)
Growth (%)

## Slide 7: CERAMICS INDUSTRY
Household ceramics
Decorative ceramics
Construction ceramics
Art ceramics
Types of Vietnamese ceramic
Sanitary ware
Technical ceramics

## Slide 8: CERAMICS INDUSTRY
Stages in the ceramic production process
Introduce:
• Ceramic is a traditional handicraft product, produced through many meticulous stages.
• The ceramic production process combines traditional techniques and modern improvements, with the ingenuity of the craftsman.
The ceramic production process includes 7 main stages:
1. Raw material extraction and processing.
2. Product shaping.
3. Drying.
4. Decoration and glazing.
5. Initial firing.
6. Product finishing.
7. Inspection and packaging.

## Slide 9: CERAMICS INDUSTRY
Step 1 - Raw material exploitation and processing
Raw materials: Clay, kaolin, quartz, feldspar.
Exploit: Choose the right type of clay, free of impurities; Let the soil "incubate" to increase plasticity.
Processing: Grind the raw materials; Mix the soil with water and additives to create a homogeneous mixture. Various machineries could be used in the processing depending on the capacity and types of products including: Grinding machine, sieving machine, mixing machine, spray dryer etc where as spray drier could consume large amount of Heat energy.

## Slide 10: CERAMICS INDUSTRY
Step 2 - Product shaping
Shaping techniques:
  Hand molding: Suitable for artistic products.
  Using a turntable: Use for household items such as bowls, cups, vases.
  Molding or casting: Creating mass products such as statues and reliefs, sanitary wares,
  Compressed: to produce tiles,
Require:
  Ensures correct shape, no distortion.

## Slide 11: CERAMICS INDUSTRY
Step 3 - Drying
Purpose: Remove moisture before firing.
Method:
Natural drying: Under the sun, suitable for dry weather and for small enterprises.
  Artificial drying: Using a dryer, saves time and is more effective and normally using for factories that produce a high quantity of similar product. The driers could be in following Technologies:
      Continuous drying (tunnel drier)
      Batch drying (drying chamber)

## Slide 12: CERAMICS INDUSTRY
Step 4 - Product decoration
Rough decoration:
  Carve, emboss or print patterns directly onto the product.
  Using the underglaze painting technique, creating unique features for each product.
Tool: Paintbrush, carving knife, pattern pen, printers
Characteristic: Decorative patterns reflect the cultural and technical characteristics of each craft village for the house hold or art ceramic. In construction ceramic, the decorative normally printed

## Slide 13: CERAMICS INDUSTRY
Step 5: Glazing
Glazing:
  The product is either dipped into liquid glaze or sprayed with glaze onto the surface. In factories, glazing tiles could be a machine of both glazing and printing in one.
  The glaze provides a glossy finish, protects the product, and enhances its aesthetic appeal.
Type of glaze:
  Colored glazes: Blue, brown, white, and jade glazes.
  Transparent glaze: Maintains the original color of the product.
Require:
  The glaze should be even, without lumps or streaks.

## Slide 14: CERAMICS INDUSTRY
Step 6 - First firing of the product
Kiln: There are various types of kilns for firing process. Traditional kilns (wood-fired or coal-fired) or modern kilns (gas or electric) are used. To produce construction ceramic, sanitary wares, technical ceramics, the tunnel kiln or Roller kiln
Firing process: Firing process require a carefull control of the temperature for each step of firing. Normally, the product should increase temperature in a controlable period until it reached to the setting temperature normally 800 – 1200 oC depending on the product and also slowly colling down until it could be unloaded from the kiln.
Require: Stable temperature, no thermal shock causing product cracking.

## Slide 15: CERAMICS INDUSTRY
Step 7 - Finishing the product
Finishing after firing:
  Polish and smooth the surface if necessary.
  Add additional decoration by hand painting or decal printing.
  Grinding to ensure accurate dimensions for technical porcelain and sanitary porcelain products
Check: Reject defective products: cracks, uneven glaze or non-standard shape.
Packing: Qualified products are packed into bales for easy shipping.

## Slide 16: Folk and fine arts Ceramic production process
The preparation of raw materials requires a variety of streamlined raw materials. The mixing requires precision and ensures plasticity, smoothness, electricity consumption or manpower for kneading The shaping can have many methods that need to be aesthetic. The drying of the product needs to control the drying process appropriately to avoid cracking and damage to the product Glazing helps the product get the right color The process of heating the main energy-consuming product needs to be considered for optimization. The firing needs to adjust the firing curve precisely to ensure product quality

## Slide 17: GRANITE/PORCELAIN TILE PRODUCTION TECHNOLOGY
Annotation: | 
(1) Feeding conveyor (2) Lump crusher (3) Weighing raw materials (4) Conveyor (5) Funnel (6) Conveyor (7) Ball mill (8) Vibrating sieve (9) Agitation pit (10) Diaphragm pump (11) Transfer tank (With vibrating sieve) (12) Spray drying tower (13) Clay powder silo tank (14) Conveyor (weigher) | (15) Hopper for raw material for press (16) Powder feeding table (17) Hydraulic press (18) 5-layer drying oven (19) Glazing and printing line (20) Greenware storage (21) Kiln (22) Finished product storage (23) Edge grinding and polishing line (24) Sorting and packing (25) Vibrating sieve
Granite/porcelain tile production technology

## Slide 18: SANITARY CERAMIC PRODUCTION PROCESS
RAW MATERIALS
CASTING
GLAZE SPRAYING
TUYNEL KILN
CHECK
PACKAGING SHIPMENT
SHAFT KILN
WASTE LAGOON
FAILED
FAILED

## Slide 19: HIGH QUANTITIES FACTORY FOR CERAMIC PROCESSING
For the factories produce high quantities of similar product such as sanitary ware, tiles technical ceramic, or household ceramic. There are many energy consumption process in the factory including:
  Compressed air producing for different purposes of production process.
  Conveyors to transfer materials.
  Pumps for transfer the slurried materials.
  Raw materials milling and seaving to ensure the materials quality.
  Spray drier consume a large amount of heat energy for water evaporation.
  Drying kiln consume a high amount of heat in the form of fuel consumption.
  Firing process in the kiln consume highest amount of Heat energy in the form of fuel consumption.
  Normally, fuel used in the facilities is gas such as LPG; CNG or gas produced by coal gasifier. In some cases, the gasifier could use Biomass as a fuel.

## Slide 20: TYPES OF KILNS FOR CERAMIC PRODUCTS
Tunnel Kiln for Ceramics
Shuttle Kiln for Ceramics
Roller Kiln for Tile Firing

## Slide 21: BRICK PRODUCTION PROCESS USING TUNNEL KILN
Excavated clay material
Open-air clay stockpile for weathering
Covered indoor clay storage
Coarse rolling
Coarse rolling
Dry mixing
Fine rolling
Kneading with a sieve and water spraying to stabilize moisture content
Vacuum kneading-extrusion combined process
Drying yard
Automatic tile cutting
Tunnel drying oven
Tunnel Kiln
Classification and storage of finished products
Coal crusher
Coal warehouse
Coal feed hopper

## Slide 22: BRICK PRODUCTION PROCESS USING TUNNEL KILN
Fired brick production is a type of production that consumes a lot of energy on the following factors
  Soil material needs to be exploited, stored, stirred and weathered for a long time. Machine tools such as excavators, bulldozers, etc. need to be used for this stage. Water also needs to be used to promote weathering to improve quality. Many machines used in the line have power consumption including barrel feeders, coal crushers, twin-shaft kneading machines, rolling machines, combined vacuum extruders, cutting machines. The new lines follow the trend of using drier raw with a semi-dry extrussion process that reduces the need for drying. Factories have also made many improvements and modernizations with the use of robots for brick picking, stacking bricks into trolleys to enter the kiln or stacking bricks directly in the kiln The calcining process consumes a lot of fuel, mainly low-quality coal, boiler ash, still carbon, etc. The stacking of finished bricks out of the oven also tends to use robots

## Slide 23: SOME BASIC EQUIPMENT IN BRICK PRODUCTION LINE
  Hopper Feeder
Conveyor
Rolling mill
2-shaft kneading machine
Continuous Vacuum Kneading-Extrusion Machine
Automatic Brick Cutter

## Slide 24: PRODUCT DRYING PROBLEM
Covered drying yard
The drying kiln is placed next to the tunnel kiln to utilize the kiln heat for the drying process.

## Slide 25: TYPES OF KILNS FOR CONSTRUCTION BRICK PRODUCTS
Mobile Tunnel Kiln with Flat Roof
Mobile Tunnel Kiln

## Slide 26: GENERAL ON THE PRODUCTION PROCESS OF BRICK/CERAMIC FROM CLAY
The main raw material is clay with different quality grades. In addition, other components such as feldspar, kaolin, quartz, ceramic glaze and other additives are also used depending on the type of product being produced.
There are many mechanical steps used to transform and improve the properties of raw materials including grinding, rolling, filtering, etc. to increase the smoothness, plasticity and mechanical properties of the raw materials, making the product shaping process easier and improving the mechanical properties of the product. These steps consume a lot of electricity for machine tools and conveyor systems.
The product shaping stage can have many methods such as pressing, casting, manual shaping
The decoration or surface feature creation stage such as glazing, drawing, coloring helps the surface to have the desired artistic properties.
The drying/drying stage helps to separate moisture and partially drain water. This stage needs to be carried out carefully with a controlled drying speed to avoid cracking and breaking the finished product. The firing stage is carried out in kilns to transform the product properties into a solid form through the process of solidification when fired at high temperatures up to 1000℃
The firing process requires close monitoring of the temperature increase rate as well as the temperature decrease rate to avoid cracking and breaking the product.

## Slide 27: BRICK PRODUCTION TECHNOLOGY
Current types of manual production technology are difficult to survive, are not allowed to operate and are gradually being eliminated.
The type of large-capacity Hoffmann kiln technology still exists due to low investment costs, high production capacity with good competitiveness. However, the technology also pollutes the environment for workers and has a high rate of defective products due to poor combustion control.
There are 3 types of tunnel kiln technology including:
  Tunnel kiln with narrow ceiling. This technology is usually old kilns, low efficiency and high fuel costs, poor combustion control.
  Flat ceiling tunnel kiln with wide furnace. This technology is newer with a ceiling structure made of refractory ceramic wool, easy to control, larger capacity and more fuel efficient.
  Moving tunnel kiln technology has a kiln structure made of refractory insulating ceramic wool that can move in a circle while the bricks stand still. This technology imported from China has a large capacity, a variety of fire adjustment modes, so it produces higher quality bricks. The production system is integrated with a brick-picking robot, so the production process can be optimized. The flat-ceiling moving tunnel kiln technology has a rectangular structure with a movable refractory ceramic wool ceiling, creating a cavity to help the robot pick up bricks and arrange them in the kiln for continuous production.

## Slide 28: ENERGY USED IN THE BRICK AND CERAMIC INDUSTRY
Electricity is used a lot for the stages of the production line with the use of a variety of crushing, rolling, chopping, pumping, fan, conveyor belts, etc.
Fuel consumption plays a very important role in heating the product to high temperatures. For construction bricks and raw ceramics, coal plays the main role as fuel.
For glazed ceramic products, gas fuel is commonly used.
The drying stage is often integrated with the firing stage, whereby the heat utilized from the firing stage contributes significantly to drying, helping to save energy. A clear analysis of the heat utilization factor at each step for the drying, heating, firing, and cooling stages helps to improve energy saving and reduce the rate of waste products.
In some cases, factories are equipped with a coal gasification system to convert coal into gaseous fuel with the main component being CO, helping to reduce fuel costs compared to using gas.
There are three types of kilns commonly used, including shuttle kilns that fire intermittently in batches for the production of household ceramics; tunnel kilns used for a variety of ceramic products, and roller kilns that are more commonly used for tiles and roof tiles. The roller kiln type offers greater energy savings than the other two types of kilns.

## Slide 29: Concrete brick production process

## Slide 30: The production process of concrete bricks
Concrete brick or aggregate cement is a type of brick produced from raw materials including cement, sand, mite or small gravel, water, and additives for concrete bricks and cement, sand, mite stone, ash and slag, or industrial waste (coal slag, stone mite) for aggregate cement bricks. The production process is quite simple, including mixing the raw materials in the right amount, pressing them into a forming mold to produce brick products, and curing on a large field for a suitable amount of time for cement and aggregates to be bonded and hardened. An important point in the production system is the ability to accurately quantify the raw materials and the ability to mix evenly to ensure that the adhesive (cement) is uniform throughout the block and binds to all other aggregate components. The arrangement of silos containing raw materials, weighing scales, and mixers plays an important role in the production process Forming presses also play an important role in obtaining quality assurance products. The hydraulic type static press for bricks has high smoothness, large pressing force but the capacity is not guaranteed while the vibrating press gives higher output but the pressing force will be lower. The maintenance work requires the factory area to have a large land area due to long-term maintenance.

## Slide 31: AAC production process
Process of an AAC lightweight concrete production chamber

## Slide 32: AAC production process

## Slide 33: AAC production process
Material. Cement (or lime), Gypsum, Fine sand (or fly ash, furnace slag), Aeration agents: Aluminum powder (Al) or aluminum compound, Water and additives (enhance strength, plasticity). Raw materials are accurately weighed and quantified to ensure quality. Mix the mixture. The dry ingredients (cement, sand, gypsum) are mixed well in the mixer, Add water to make a liquid mixture (slurry); Aluminum powder is added last. The reaction between aluminum powder and lime (or cement) in an alkaline environment produces hydrogen gas. Hydrogen gas creates small air bubbles, which cause the mixture to expand, increase in volume, and form a porous product. Hydrogen gas creates small air bubbles, which cause the mixture to expand, increasing in volume. Die casting. The mixture after hatching is poured into large molds. The incubation process takes place in 30-60 minutes, creating an even bubble structure. The mixture begins to solidify slightly, reaching a "semi-solid" state

## Slide 34: AAC production process
Shaping Cutting. After preliminary solidification (usually 2-4 hours), the concrete block is removed from the mold, Use steel wire or a specialized cutter to cut into standard-sized bricks or slabs. The cutting process ensures high precision, flat surface. Autoclaving. The bricks are fed into the autoclave. Stay in a saturated steam environment at high pressure (8-12 bar) and 180-200°C for 8-12 hours. This process strengthens the chemical bonding, improving the strength and stability of the tile. The air bubble structure is fixed, creating a lightweight and durable product. Cool and pack. After autoclaving, the bricks are cooled gradually to avoid cracking. Finished bricks are checked for quality (durability, size, water absorption). Packed and stored, ready for distribution.

## Slide 35: General of non fired brick industries
Eventhough there are several types of non fired brick to replace the fired brick for construction, there are only 2 types could be developed including Concrete brick and AAC
Energy consumption of concrete brick mostly in the form of electricity for the compressed machines and some other machines such as mixing machine, conveyor. In case of replacing fired brick, non fired brick already save a significant energy saving due to lack of firing process.
Changing sharp of the concrete brick could also save energy instead of using the brick sharp similar to the fired brick.
In many case brick quality is low due to lack of investing on the automatic weighing scalesvà mixing machine to have homogeneus blending system.
The compressing machine may use server motor for more saving energy.

## Slide 36: General of non fired brick industries
AAC is light construction materials which can have a good thermal and sound insulation however, High water permeability requires special way of construction technique that can prevent the water absorbtion.
Since AAC is light construction material for that it have lower requirement of concrete frame structure. However, the designer in Vietnam still design the house or building with heavy concrete frame structure. The improvement of design from begining could save concrete frame materials of building and houses.
Production of AAC require significant amount of steam at high pressure and temperature. However, many of them using steam system that condensate recovery at atmospheric pressure. By improving steam system into high pressure condensate recovery, significant energy could be saved in the form of steam.

## Slide 37
THANK YOU!