## Slide 1
Module 8.5:
Energy efficiency opportunities in brick and ceramic production lines.
Technical staffs
TRAINING PROGRAMME FOR INDUSTRIAL ENTERPRISEs

## Slide 2: CONTENT
CHARACTERISTICS OF ENERGY USE IN THE PRODUCTION OF BRICK AND CERAMIC.
ENERGY EFFICIENCY MEASURE IN BRICK AND CERAMIC.
OTHER ENERGY SAVING OPPORTUNITIES IN CERAMIC PRODUCTION

## Slide 3: 1. ENERGY IN BRICK PRODUCTION (1)
Fired bricks are a type of raw ceramic product used in construction. The main energy used includes
Electricity is used for machines in the shaping processing line, fans, brick inlet and outlet equipment in the kiln.
The fuel, mainly coal, is used in the brick firing process. In Vietnam, coal is often mixed with soil during the shaping processing and a part is sprinkled outside to adjust the temperature in the main firing zone in the kiln.
The main types of kilns used today include ring kilns, tunnel kilns, moving tunnel kilns, and flat ceiling moving tunnel kilns.

## Slide 4: 1. ENERGY IN BRICK PRODUCTION (2)
The stages in the brick kiln firing process include:
Drying stage. After being processed and shaped, the raw bricks can be exposed to the sun, dried in the kiln, and when put into the kiln, the raw bricks are dried at a low heating temperature. the drying speed is adjusted appropriately to avoid cracking and breaking the product during the drying process. In general, the drying stage can raise the brick temperature to 120°C.
Heating stage. This is done by gradually raising the brick temperature; at this time, some organic components can be released, the temperature is raised to about 500°C, and the crystalline moisture can be released.
Firing stage. This is done by raising the brick temperature to the temperature of the block, with the phase change of the soil into ceramic form. Depending on the soil quality, the specific needs of the market for brick color, this temperature can be from 800 - 1000°C.
Cooling stage. It is done by cooling the bricks gradually at a suitable rate to avoid sudden cracking of the bricks.

## Slide 5: The firing curve describes the progression of the brick firing process
Green brick
Flue gas
Preheating
Firing
Cooling
Firing curve
Sulfur
Volatile matter
Chimney
      1. ENERGY IN BRICK PRODUCTION (3)

## Slide 6: FIRING CURVE IN A TUNNEL KILN
      1. ENERGY IN BRICK PRODUCTION (4)

## Slide 7: 1. ENERGY IN BRICK PRODUCTION (5)
Depending on the kiln technology, the drying, heating, firing, and cooling stages can utilize heat from each other, including:
The heat that needs to be released from the cooling stage can partly support the drying process and partly heat the air supplied to the fuel combustion process.
The fuel combustion process uses hot air from the previous cooling process to help the bricks raise their temperature to the condensation temperature in the firing zone.
The smoke generated in the firing zone after being used to fire the bricks, while the high temperature will be used to slowly raise the brick temperature in the heating zone and then the excess heat will be supplied to the drying zone and then exhausted through the chimney.
With some kilns integrated with the drying furnace right next to it, the hot smoke ducts from the end of the drying zone of the kiln and the hot air ducts from the cooling zone will be designed to provide appropriate heat to the drying furnace.

## Slide 8: Using the new kiln technology that can save energy
There are many kilns with low energy efficiency are in operation in Vietnam including narrow tunnel kiln with arch roof; Hoffmann kiln with backward technology. The new model kilns should be:
  The flat roof tunnel kiln using ceramic wool compressed for the roof that can reduce heat loss through the roof.
  Mobile tunnel kiln for that whole the kiln is constructed by light insulation materials that could be moved in the circle and bricks stacked at the floor and will be fired when the kiln move through
  Moveable roof tunnel kiln where as the kiln is costructed with only the roof could be moved. Brick is stacked at the floor and the fire move with the move of the roof.
Energy saving could be up to 30% by changing technology as well as the production capacity
EEMS IN BRICK PRODUCTION

## Slide 9: EEMS IN BRICK PRODUCTION
Tunnel kiln with the narrow tunnel and arch roof
Hoffmann kiln

## Slide 10: EEMS IN BRICK PRODUCTION
Mobile Flat Roof Tunnel Kiln
Mobile Tunnel Kiln

## Slide 11: EEMS IN BRICK PRODUCTION
Using new Technologies for the production process including:
  Using robot for brick stacking and brick unloading can help to optimize airodynamic in the kiln and reduce mistake of labor stacking brick.
  Using the dry process of brick forming for that the brick formation is already dry compare to wet process. The Energy used for evaporation of water could be reduced significantly.
  Improve drying method. At present, many brick company using the in efficiency drying under the clear roof to use the solar Energy for drying. However, the bad arrangement of brick stacking can reduce efficiency of drying process for that it can increase Energy used for water evaporation as well as reduce the production of the factory. Improvement of drying process could be a oppotunities of Energy saving.
  Using inverter to control Fan motors. There are many kilns Using dampers to regulate airflow leads to high energy consumption. Using fan motor may reduce electricity consumption
  There will be significant Energy could be saved by checking and improve the insulation of various place of the kiln such as a roof, flue gas tube or hot air driven tubes.

## Slide 12
Check for factors that affect the operation of the kilns
Factors that are easy to cause leaks, Not properly designed and equipped. Leak between kiln car causes heat loss through the bottom of tunnel kiln
EEMS IN BRICK PRODUCTION
The cushions at the points of contact of the trolley need to be sealed 100%. The outer ceramic layer must retain its elasticity.
The steel armor of the wagon must be flat and neat at the wagon's impact points.
The sand sealing positions must be completely filled with sand

## Slide 13: EEMS IN BRICK PRODUCTION
Light Kiln Car
Kiln cars in Vietnam are often neglected, resulting in heavy weight due to construction with many heavy refractory bricks, leading to frequent damage and the need for repairs.
The main cause is poor construction quality, the use of substandard mortar, and improper handling, especially when cleaning the kiln car after removing bricks from the kiln. During this process, dust from the kiln car accumulates in the mortar joints, gradually loosening the brickwork of the kiln car.
The experience from other countries suggests using industrial vacuum cleaners to clean the kiln cars, which not only prevents dust exposure for workers but also helps maintain the car's durability.
When the kiln car is heavy, it accumulates a large amount of heat, taking longer to cool, which affects the productivity of workers who load bricks onto the car.
Thus, having a lightweight kiln car structure helps to:
Energy efficiency
Improve labor productivity
Enhance working conditions for workers.

## Slide 14: EEMS IN BRICK PRODUCTION
Reduce heat loss to the environment:
The kiln wall structures and the gas/smoke ducts from the firing chamber to the drying chamber are large structures that are exposed to high temperatures and radiate significant heat.
As a result, they cause heat loss and negatively affect the working conditions of kiln operators.
In general, most facilities apply insulation to these high-heat structures; however, many areas still suffer from significant heat loss.
Today, there is a wide availability of thermal insulation materials on the market.
Facilities should implement better insulation and aim for a surface temperature of 60°C for these structures to minimize heat radiation into the working environment.

## Slide 15: EEMS IN BRICK PRODUCTION
Renovation and Adjustment of Gas/Smoke Flow in the Tunnel Kiln System
Renovating and adjusting the gas/smoke flow system in the firing and drying kiln is a challenging task that requires the consultant or implementer to have a solid understanding of drying processes and efficient heat utilization.
For many production facilities, this presents a significant opportunity for energy savings.
The following basic guidelines can be used as a reference when adjusting the gas/smoke system for the firing and drying kiln:
  The typical ratio of gas mass exiting the kiln to brick mass is 3 kg of gas per 1 kg of brick.
  In Vietnam, this ratio is often slightly higher due to the use of coal as fuel, but it should not exceed 4 kg of gas per 1 kg of brick.

## Slide 16: EEMS IN BRICK PRODUCTION
Renovation and Adjustment of Gas/Smoke Flow in the Tunnel Kiln System
The exhaust gases exiting the drying chamber should be controlled using a frequency inverter to ensure that the volume of incoming air is balanced with the outgoing air, thereby preventing cold outside air from entering the kiln.
Priority should be given to extracting hot air from the cooling zone for use in the drying process, which can help reduce the volume of exhaust gases released from the kiln.
A rapid cooling system should be used to extend the cooling time as the bricks pass through the quartz transformation zone.
It is important to properly regulate the airflow during rapid cooling to ensure the required cooling temperature is maintained. Many enterprises operate this system improperly, resulting in brittle bricks.

## Slide 17: EEMS IN BRICK PRODUCTION
Replace fired brick by non fired brick. Non fired brick reduce Energy consumption to produce one volume of construction materials since it can avoid the firing process in the kiln.
The production of bricks from aggregate concrete will include mixing raw materials (cement, aggregates such as sand/gravel, water, additives), molding/vibration compression, curing, and storage/transportation. The industry consumes energy primarily from electricity (for mixers, vibration compression) and heat (for steam maintenance), accounting for 20-40% of production costs, with the potential for savings of 15-50% through optimization and recycled materials
The production process of non-fired aggregate concrete bricks should be energy-saving, focusing on reducing electricity consumption for mixers and compression vibrators, as well as optimizing production schedules. In large factories, training employees for efficient operation, combined with automation systems (IoT) for real-time energy monitoring, reduces electricity consumption by 10-20% for compression vibration

## Slide 18: EEMS IN BRICK PRODUCTION
Use recycled aggregates or porosizing additives to reduce energy use in production and application (such as better insulation). In aggregate concrete bricks, 20-50% RCA is used from construction waste to produce sustainable bricks, reducing overall energy by 20-40%. Lightweight tiles with perlite reduce heating/cooling energy in construction by 10-17%. Thermal power plant fly ash sources can also be used to produce aggregate concrete bricks
For the Autoclaved Aerated Concrete, energy use includes Electricity: Accounts for 30-50% of energy, used for mixing, crushing sand/fly ash, cutting, and transportation (conveyors, pumps). Heat: Accounts for 50-70%, mainly for autoclave maintenance (steam 180-200°C). Energy-saving solutions can reduce total energy by 15-40%, especially in autoclaving and mixing materials.
. Heat recovery in autoclave chamber and curring system could be 10 – 20% if the heat from condensate at high temperature could be recovered. Normally. Condensate could be recovered at high pressure at 180oC.
Using a high-efficiency mixing and crushing machine (such as Hess AAC or Wehrhahn's energy-saving ball mill) to reduce the sand/fly ash crushing time from 2-3 hours to 1-1.5 hours, reducing power consumption by 15-20%. The application of inverter to the crusher saves energy for the crushing process when adjusting the ball mill speed.
Using high-efficiency foaming additives (such as HPMC - Hydroxypropyl Methylcellulose) to reduce the amount of aluminum powder, reduce the mixing and curing energy by 5-10%. Using fly ash helps reduce the demand for cement.

## Slide 19: ENERGY USAGE IN CERAMIC PRODUCTION PROCESS
In general, ceramic products other than fired bricks have higher requirements in terms of design, shape, and surface characteristics.
The stages of raw material processing and product forming are more complex, requiring more advanced machinery and equipment. The raw materials often have higher plasticity, and the forming processes are more diverse and detailed. As a result, electricity consumption in these stages may be higher, or the production may require more meticulous manual labor, especially in the case of artistic and household ceramics.
The drying and firing stages demand greater precision in the drying and firing curves. Additionally, the fuels used must avoid producing dust or tar, which could damage the product surface.
The fuels commonly used for kilns in ceramic production are gaseous fuels, such as LPG, natural gas, or gas from gasification processes that has been properly filtered and cooled.

## Slide 20: ENERGY USAGE IN OTHER TYPES OF CERAMIC PRODUCTS
Kilns used in ceramic production include:
  Various types of kilns such as the rice husk-fired dome kilns in the Mekong Delta, the wood-fired step kilns in Binh Duong, and the coal-fired vertical kilns in Bat Trang and other traditional ceramic villages in Northern Vietnam have been gradually phased out or are being eliminated due to environmental pollution and high rates of broken or defective products.
  Shuttle kilns using LPG and operating in batch mode have been increasingly adopted by ceramic manufacturing enterprises. In general, small-scale production in traditional craft villages in the North relies on small shuttle kilns with capacities ranging from 9 to 18 m³. Meanwhile, enterprises in the Binh Duong area operate large-capacity shuttle kilns of up to 230 m³, enabling high-volume production and significantly reducing specific heat consumption.

## Slide 21: ENERGY USAGE IN OTHER TYPES OF CERAMIC PRODUCTS
Types of Kilns Used in Ceramic Production (continued):
  Enterprises producing sanitary ware products (such as washbasins, toilets, etc.) typically have large and stable production volumes, and therefore often use tunnel kilns fired with LPG or product gas from coal gasification. In general, tunnel kilns used for firing sanitary ceramics have kiln cars designed with much lighter materials compared to those used in tunnel kilns for brick production. However, significant heat losses still occur through kiln furniture (such as setting supports) and the kiln cars themselves. Since the fuels used are expensive, reducing heat loss can result in substantial cost savings.
  Manufacturers of glazed ceramic tiles usually use roller kilns fired with LPG or gasified coal. Roller kilns do not use kiln cars, which helps eliminate a major source of heat loss associated with kiln cars and kiln furniture.

## Slide 22: EEMS IN CERAMIC PRODUCTION
A thorough investigation of electrical equipment structures provides significant energy savings with the use of frequency converters for fans, pumps, various types of grinders, and conveyors.
With the use of multiple input materials in the form of blending in different blending processes, energy mapping provides a great opportunity for overall management in the chain to reduce material loss and improve overall production efficiency.
The drying stage has many diverse drying methods including spray drying, batch drying chambers, tunnel kilns or rollers that utilize heat from the kiln, providing great energy savings potential when the heating process for each stage is carefully investigated and optimized.

## Slide 23: EEMS IN CERAMIC PRODUCTION
As with brick production, the majority of energy used with high energy costs is concentrated in the kiln with the following energy saving opportunities:
Survey, energy balance for the kiln and study the heat losses to reduce heat losses and optimize the firing process. Solutions for brick kiln tunnels can be considered for appropriate application.
Research on optimizing the coal gasification system.
Research on utilizing heat to dry the air before supplying it to the gas combustion process at the nozzle.
Research on utilizing excess heat from the kiln to gasify LPG.

## Slide 24: EEMS IN CERAMIC PRODUCTION
For businesses using batch-fired shuttle kilns, at the end of the kiln firing process, the exhaust temperature is often very high (300 – 600°C) and cannot be utilized. Researching and building a drying kiln that utilizes heat from the kiln or operating 2 or more connected kilns can help utilize the excess heat from the previous kiln for drying or heating the next kiln.
At times when electricity is cheaper than LPG, some businesses have designed a system to raise the kiln temperature to about 700°C using electricity and to raise the temperature from 700°C to about 1000 – 1100°C using LPG.
In the production of paving tiles and building ceramics, the heat recovery from the furnace cooling air to dry the raw materials or heat the water, can save 10-30% of the overall energy.
Use waste heat to preheat the drying air or reuse it in the molding process, reducing energy by 15-25%.
Using recycled glass in ceramic production to partially replace clay can reduce firing energy by up to 50% compared to clay-based ceramics, which is especially suitable for household and technical ceramics. The reason is that recycled glass with a lower firing temperature will help reduce the firing temperature required for the ceramic product.

## Slide 25: EEMS IN CERAMIC PRODUCTION
Changing the material formula to reduce the firing temperature, such as using recycled additives (fly ash, waste glass) in tiles and building ceramics, reducing the firing energy by 20-37%. For technical ceramics (such as electronic or medical ceramics), using advanced materials such as granite slabs can reduce water and energy consumption by up to 50% compared to traditional clay, and improve technical properties.
Adopt a high-efficiency kiln (such as a roller kiln with thermal oil) to optimize heat distribution during the kiln stages and take advantage of the spray drying process, reducing energy by 10-25% compared to traditional kilns.
Implement Energy Management Systems (EMS) in accordance with ISO 50001, incorporating AI to monitor and optimize real-time consumption. In large factory, this can save 15-20% without large investment.
Application of renewable energy and cogeneration of Thermal power for plants. Currently, some factories use biomass gasification technology to generate gas instead of coal gasification provided for the calcination process. A process of cogeneration of thermal power with gas fuel has been studied and applied by Italy to optimize the use of gas to both generate electricity and heat for the furnace. The biomass gasification process combined with cogeneration can also be applied to bring high efficiency for energy saving. Ceramic factories usually have a large area, so there are many opportunities for the installation of rooftop solar power systems.

## Slide 26: EEMS IN CERAMIC PRODUCTION
Using AI and IoT to monitor kilns in building tiles and ceramics, reducing heat waste by up to 20%. For technical ceramics, 3D printing technology reduces excess material and injection molding energy Implement a digitalization system (Industry 4.0) to predict maintenance and optimize production lines. In large factory, this can save 10-20% which is lower cost than equipment replacement Applying energy-saving furnaces with automatic control with advanced insulation materials, making the most of waste heat with the application of heat loading oil to reduce consumption by 20-30%.
Optimize the heat used in existing coal gasifiers by taking advantage of the excess heat from the gas cooling process from the gasifier to heat the inlet air which saves 5-10% of fuel and produces gas with a higher calorific value.

## Slide 27
THANK YOU!