## Slide 1: TRAINING PROGRAMME FOR IEs
MANAGEMENT OFFICERS
Module 8:
Energy efficiency opportunities in steel production lines.

## Slide 2
STEEL PIPE AND GALVANIZED STEEL MANUFACTURING INDUSTRY

## Slide 3: CONTENT
1. Energy Saving Opportunities in the Blast Furnace (BF) Process
2. Energy Saving Opportunities in the Electric Arc Furnace (EAF) Process
3. Other Opportunities
Notes: Hợp đồng hiệu quả năng lượng (EPC): là hợp đồng ký kết giữa ESCO và Khách hàng để thực hiện dịch vụ sử dụng năng lượng tiết kiệm và hiệu quả.
– Hợp đồng chia sẻ mức tiết kiệm năng lượng: ESCO chịu mọi rủi ro tài chính và kỹ thuật của dự án bằng cách thu xếp tài chính để thực hiện dự án đầu tư lắp đặt các trang thiết bị hiệu quả năng lượng tại cơ sở sử dụng năng lượng của khách hàng
– Hợp đồng đảm bảo mức tiết kiệm năng lượng: ESCO chịu trách nhiệm cung cấp, thiết kế, lắp đặt, đo lường và đảm bảo hiệu quả giải pháp sử dụng năng lượng tiết kiệm và hiệu quả cho khách hàng.

## Slide 4
1. ENERGY EFFICIENCY OPPORTUNITIES IN THE BLAST FURNACE (BF) PROCESS
The Blast Furnace (BF) process is one of the traditional steel production methods. To reduce costs and greenhouse gas emissions, energy efficiency is crucial. Solutions include optimizing raw material inputs, improving blast furnace gas efficiency, enhancing the use of pulverized coal injection, and utilizing waste heat.
The use of high-quality iron ore, increased use of sintered pellets, and blending coke with pulverized coal can help reduce coke consumption by 10-15%. TRT technology can recover 20-40 kWh per ton of pig iron.
TRT: Top-pressure Recovery Turbine – a system of turbine system that recovers the top pressure of the blast furnace after the iron smelting process

## Slide 5
1.1 OPTIMIZING INPUT MATERIALS
Raw materials in blast furnace
The main raw materials used in blast furnaces for steel production include:
Iron ore: Is the main raw material, providing iron for the steel production process.
Coke: Provides carbon for the iron ore reduction reaction, which helps create iron and high temperatures in the blast furnace.
Lime (CaO): Used to remove impurities such as silica in iron ore.
Additives: Include materials such as limestone, dolomite, other minerals to adjust the properties of steel.
To optimize raw material inputs in the blast furnace process, it is essential to focus on using high-quality iron ore with high Fe content and low impurities. This helps reduce coke consumption and the energy required for ore reduction. In addition, increasing the use of high-porosity pellets and sinter enhances the reduction efficiency within the furnace.
Another solution is blending coke with Pulverized Coal Injection (PCI) to reduce coke consumption. This approach not only helps lower production costs but also decreases dependence on coke, a resource that is becoming increasingly scarce.

## Slide 6
Optimizing input materials solution
Improve raw material quality: Ensures consistent quality of input materials, removes unwanted impurities, improves material smoothness, and increases reaction efficiency in the furnace.
Adjust the mixing ratio of raw materials: TThe ratio between iron ore, coke and additives needs to be flexibly adjusted to optimize blast furnace performance, ensuring there is no shortage or excess of raw materials, affecting product costs and quality.
Use alternative materials: Using alternative feedstocks such as biochar, industrial waste, or steel scrap can reduce input material costs and reduce CO₂ emissions.
Optimize the air flow in the furnace: Improved air supply and temperature control systems to ensure that all materials in the furnace reach the temperature required for chemical reactions.
Strengthening the exhaust gas recycling system: The exhaust gas from the blast furnace can be reused to power other processes in the plant, reducing dependence on external energy.
1.1 OPTIMIZING INPUT MATERIALS

## Slide 7
1.1 OPTIMIZING INPUT MATERIALS
Analysis of the influence principle of input materials
Ore
Type of ore (fine particles, lump ore, iron ore pellets) affects furnace permeability, reduction capability, and heat consumption.
Pellets or pre-heated ore help reduce the amount of heat needed for reduction → lowering coke consumption.
2. Coke:
Coal with a high CSR (Coke Strength after Reaction) helps reduce cracking in the furnace and improves heat exchange efficiency.
Optimizing coke size improves furnace permeability and thermal performance.
3. Limestone and additives:
Using high-purity limestone (CaCO₃ > 90%) enhances the impurity removal reaction → reduces excess heat generation.
Proper use of fluxing additives lowers the melting temperature → saving energy.
4. Moisture content of materials: Reducing moisture before feeding into the furnace helps minimize heat loss due to water evaporation.

## Slide 8
Ingredient | Before Optimizing (kg) | After Optimizing (kg) | Notes
Iron ore (58% Fe) | 1600 | 1500 | Increase the rate of ore pellets
Coke | 500 | 450 | Due to better revert
Limestone | 200 | 180 | Increase Altitude more efficiently
Heat Consumption | 13 GJ | 11.5 GJ | Due to a more efficient reaction
Preliminary calculation of potential energy savings
Input assumptions for 1 ton of cast iron:
1.1 OPTIMIZING INPUT MATERIALS

## Slide 9
Energy Saving:
Energy reduction:
Reduction rate: ~11.5%
Calculate your savings (for example):
Assuming a factory produces 1,000,000 tons of cast iron per year:
Energy saving/year:
Converted to fuel costs: If coke costs $100/ton, 1 ton of coke = 28 GJ
→ Tiết kiệm ~5,35 triệu USD/năm
1.1 OPTIMIZING INPUT MATERIALS

## Slide 10
Implementation recommendations
Use blast furnace simulation software (e.g., BF Simulator, FactSage) to evaluate the optimal composition.
Invest in input material drying systems to reduce moisture content.
Conduct regular quality checks on raw materials (Fe%, moisture, particle size).
Optimize burden mix using AI or real-time blending algorithms.
1.1 OPTIMIZING INPUT MATERIALS

## Slide 11
1.2 Improving Blast Furnace Gas Efficiency (Top Gas Recovery)
Overview of Blast Furnace Gas (BFG):
Composition: ~20–25% CO, ~3–5% H₂, ~15–20% CO₂, with the remainder being N₂ and inert gases.
Calorific value: ~3,000–4,000 kJ/Nm³ (very low compared to natural gas: ~39,000 kJ/Nm³).
Commonly reused in:
Boilers (for steam generation)
Reheating furnaces (to heat metal)
Turbines (for power generation if sufficiently pressurized)
Common Issues to Be Improved:
Low gas recovery efficiency due to leakage and poor cleaning.
Non-optimized burner systems → incomplete combustion of CO.
Lack of synchronization between gas generation and actual usage demand.
No buffer gas storage system, leading to excess gas being vented.

## Slide 12
Context and Existing Issues
Blast Furnace Gas (BFG) accounts for approximately 20–30% of the input energy in the pig iron production process.
Many steel plants in Vietnam, such as Hòa Phát, Formosa Hà Tĩnh, and TISCO, have not fully utilized the thermal and energy potential of BFG, leading to:
Low combustion efficiency (calorific value ~3,000–3,200 kcal/Nm³)
Excess gas is flared or not optimally recovered
Environmental pollution and wasted fuel costs
Implementation in Vietnam
Formosa Hà Tĩnh: has implemented a power generation system using BFG (Gas Turbine + HRSG)
Hòa Phát Dung Quất: uses BFG for drying systems, sintering, and power generation
TISCO: is researching upgrades to the gas cleaning system and reuse of blast furnace gas
1.2 Improving Blast Furnace Gas Efficiency (Top Gas Recovery)

## Slide 13
Solutions to Improve Blast Furnace Gas (BFG) Utilization Efficiency
Increase the reuse rate of BFG
  Before improvement: 60% of generated gas was reused
  After improvement: Reached 85–90%
Install preheating systems for hot blast using BFG
  Enhances heat exchange efficiency
  Reduces coke consumption in the furnace
Integrate a Blast Furnace Gas Turbine (BFGT): Enables power generation with ~25–30% efficiency
Optimize the BFG combustion chamber
  Maintain optimal combustion conditions (air-to-fuel ratio, temperature, pressure)
  Automate combustion control systems using PLC or DCS
1.2 Improving Blast Furnace Gas Efficiency (Top Gas Recovery)

## Slide 14
Preliminary calculation of potential savings
Input Assumptions:
Gas production: 1,500 Nm³/ton of cast iron.
The plant produces 1,000,000 tons of cast iron/year → 1.5 billion Nm³/year.
BFG Thermal Value: 3,500 kJ/Nm³.
1. Total energy in BFG/year:
2. Pre-improvement: 60% reusable → energy efficiency: 0.60×1,458=875GWh
3. After improvement: 90% reusable → energy efficiency: 0.90×1,458=1,312GWh
✅ Differential energy recovery: 1,312−875=437GWh/year
1.2 Improving Blast Furnace Gas Efficiency (Top Gas Recovery)

## Slide 15
Cost Savings Conversion
If BFG is converted into electricity using a BFG turbine at ~30% efficiency, the output would be: 437 GWh × 30% = 131 GWh of equivalent electricity
→ At an average industrial electricity price of 0.08 USD/kWh: 131 × 10⁶ × 0.08 = 10.48 million USD/year
Chỉ tiêu | Trước cải thiện | Sau cải thiện | Lợi ích
Tỷ lệ tái sử dụng BFG | 60% | 90% | +30%
Năng lượng tái sử dụng | 875 GWh | 1.312 GWh | +437 GWh
Giá trị tiết kiệm điện | – | ~10,5 triệu USD | –
Giảm phát thải CO₂ | – | ~111.000 tấn/năm | –
Summary of benefits
1.2 Improving Blast Furnace Gas Efficiency (Top Gas Recovery)

## Slide 16
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY
Replacing a portion of coke with pulverized coal injection (PCI) helps lower costs and reduce dependence on coke. This can be further combined with natural gas injection (NGI) or hydrogen injection to reduce CO₂ emissions. Each 1 kg of injected coal can replace approximately 1–1.2 kg of coke.
Increasing the oxygen concentration in the blast air improves combustion efficiency and reduces fuel consumption. When combined with pulverized coal injection (PCI) technology, it helps optimize furnace performance, leading to a 5–10% reduction in fuel use.
Technological Context in Vietnam
Major steel plants such as Hòa Phát, Formosa Hà Tĩnh, and TISCO are using traditional blast furnace technology for pig iron production.
Rising energy costs and CO₂ emission reduction targets are pushing enterprises to upgrade their technologies. The two most common and feasible solutions are:
Pulverized Coal Injection (PCI)
Oxygen enrichment in hot blast tuyere air.

## Slide 17
PCI Solution Goals
PCI (Pulverized Coal Injection) is a technology of spraying fine coal into the blast furnace instead of using coke. This helps save fuel costs, reduce coke use and increase steel production efficiency.
Mechanism of action
Fine coal (small in size and finely ground) is injected into the blast furnace, where it participates in the reduction reaction of iron ore to produce iron and other compounds.
Spray coal will partially replace coke, providing carbon for the reactions in the blast furnace without reducing steel quality..
Disadvantages and challenges
Need to invest in new equipment and infrastructure: Upgrades to the coal injection system, exhaust gas filters, and control technology are needed to ensure efficiency when using PCI.
Fine coal quality need to be tightly controlled to avoid reducing steel quality and causing blockages in the system.
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 18
The goal of the oxygen enrichment solution
Oxygen Enrichment is a solution that uses pure oxygen to replace part of the air in the steelmaking process. This helps increase the efficiency of the combustion process and improve the performance of the blast furnace.
Mechanism of action
Pure oxygen is pumped into the blast furnace instead of air, increasing the temperature and reaction rate of the blast furnace process.
The additional oxygen enhances combustion, reduces CO emissions and improves the carbon efficiency of the furnace.
Disadvantages and challenges
Invest in oxygen systems: An oxygen enrichment system with suitable capacity and precise control system is required, increasing the initial investment cost.
Oxygen quality management: Oxygen must be precisely controlled to avoid problems during production.
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 19
Technical Analysis
Basis of PCI Technology:
Pulverized Coal Injection (PCI) involves injecting fine coal into the tuyere zone of the blast furnace to partially replace metallurgical coke.
The injected coal combusts in the oxygen-rich environment, generating heat and reducing gases (CO) similar to coke.
Compared to coke, pulverized coal is cheaper and can have higher combustion efficiency if optimized properly.
Impact of Increasing PCI Ratio:
Reduces coke consumption (lower coke rate)
Lowers overall energy demand due to PCI's high calorific value (24–28 MJ/kg)
Reduces fuel costs and CO₂ emissions However, it is important to maintain proper combustion rate to avoid disrupting gas flow stability and top zone temperature in the furnace.
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 20
Preliminary Energy Saving Calculation (Assumption-based)
Assumptions:
Blast furnace output: 1,000,000 tons of hot metal per year
Current PCI rate: 100 kg PCI/ton of hot metal
Increased PCI rate: 180 kg PCI/ton (an increase of 80 kg)
Coke replacement ratio: 1 kg PCI replaces ~1.2 kg of coke
Calorific values:
  PCI: ~25 MJ/kg
  Coke: ~29 MJ/kg
  Amount of coke saved: ΔCoke = 80 × 1.2 = 96 kg coke/ton of hot metal
  Energy savings per ton of hot metal:
3. Energy savings per ton of hot metal:
784 MJ×1.000.000=784.000.000 MJ=217.778 MWh/năm
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 21
I. Technical Basis
1. Purpose of Oxygen Enrichment:
Increase the oxygen concentration in the hot blast air supplied to the blast furnace tuyeres from ~21% (ambient air) to 25–30% or higher.
This improves fuel combustion rates and raises the temperature in the tuyere zone, thereby enhancing thermal efficiency and reduction reaction rates.
2. Oxygen Supply Technologies:
PSA (Pressure Swing Adsorption): Suitable for medium-scale applications with low investment cost.
ASU (Air Separation Unit): Uses cryogenic distillation for large-scale applications.
Pure oxygen can reach concentrations of 90–99%.
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 22
Target | Reference value
Enriched oxygen levels | 25–30% O₂
Reduce coke consumption | 25–40 kg/ton cast iron
Increased blast furnace productivity | 5–10%
Reduce CO₂ emissions | 50–120 kg CO₂/ton cast
III. Energy Savings Calculation
Input Assumptions:
Production capacity: 1,000,000 tons of hot metal per year
Oxygen enrichment: from 21% → 28%
Reduction in coke consumption: ~35 kg per ton of hot metal
Calorific value of coke: ~29 MJ/kg
Efficiency of oxygen supply system: ~0.7 kWh/Nm³
II. Energy Saving Benefits
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 23
Energy savings from reducing coke
2. Energy expended to produce Oxygen (estimated)
Suppose an additional 60 Nm³ of oxygen/ton of cast iron is needed (compared to air)
Electricity consumption=60×0.7=42 kWh/ton of cast iron⇒42×1,000,000=42,000,000 kWh=42,000 MWh
3. Net Energy Savings
Δe net = 281.944−42.000= 239.944 MWh/year
1.3 ENHANCED USE OF PULVERIZED COAL INJECTION (PCI) AND
OXYGEN ENRICHMENT TECHNOLOGY

## Slide 24
1.4 UTILIZING WASTE HEAT AND NEW GENERATION BLAST FURNACE TECHNOLOGY
Recovering heat from blast furnace exhaust gases and molten slag to dry raw materials or generate electricity can reduce overall energy consumption by 5-15%. Using blast furnace slag as a construction material (e.g., in cement and concrete) helps reduce energy consumption in the production of other materials.
Hydrogen-based blast furnaces (Hydrogen-Based BF) replace a portion of coke with hydrogen (H₂) to reduce CO₂ emissions. Hybrid blast furnaces (electrified) use renewable energy to assist in ore reduction, with the potential to reduce CO₂ emissions by 20-50% when combined with green hydrogen.
Savings: Reduces overall energy consumption by 5-15%.
Lò cao số 1 tại Hòa Phát – Dung Quất

## Slide 25
Solution: Utilizing Waste Heat from Blast Furnaces for Material Drying at Hòa Phát
1. Background and Need
Hòa Phát Group is the largest steel producer in Vietnam, operating several integrated iron and steel complexes (e.g., in Dung Quất, Hải Dương, etc.).
Each complex operates large-scale blast furnaces, generating a significant amount of waste heat, particularly from blast furnace gas (BFG), reduction gas, and sintering furnace gas.
Drying input materials such as ore, sinter, and pulverized coal is a critical technical requirement to ensure efficiency and stability in hot metal production.
2. Operating Principle
Recover blast furnace gas after the dust removal and cleaning stage, utilizing its residual heat (~150–200°C).
Channel the hot gas through a gas–gas heat exchanger system or a direct drying system (e.g., fluidized bed or rotary dryer).
Materials are dried before being fed into the sintering furnace, blast furnace, or pulverized coal injection (PCI) system.
1.4 UTILIZING WASTE HEAT AND NEW GENERATION BLAST FURNACE TECHNOLOGY

## Slide 26
Estimated Efficiency at Hòa Phát Dung Quất Plant
Number of blast furnaces: 4 furnaces, each with a capacity of approximately 1,200,000 tons of hot metal per year
Total available waste heat: ~150 GJ/h across the entire system
Energy savings: >180,000 MWh/year
Reduction in DO fuel consumption: ~15,000 tons/year
Reduction in CO₂ emissions: ~46,500 tCO₂/year
Economic savings: ~12–15 million USD/year
1.4 UTILIZING WASTE HEAT AND NEW GENERATION BLAST FURNACE TECHNOLOGY

## Slide 27
2.1 OPTIMIZING RAW MATERIAL INPUTS AND IMPROVING EAF EFFICIENCY
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS
Using clean scrap (with low impurities such as copper and zinc) helps reduce melting time and energy consumption. Blending Direct Reduced Iron (DRI) or Hot Briquetted Iron (HBI) can improve energy efficiency. Preheating scrap before charging it into the furnace, utilizing waste heat from furnace gases or the cooling system to dry the scrap, reduces the energy required for melting, saving 5–15% of electricity.
Oxygen injection (Oxy-fuel burners) helps accelerate the melting rate, reducing smelting time. Using natural gas (NG) or hydrogen (H₂) as supplemental fuel can further reduce electricity consumption. Automated control systems (AI, IoT) optimize current, voltage, and electrode positioning to minimize energy losses, leading to a 10–25% reduction in electricity usage.

## Slide 28
2.1 Optimizing Input Materials and Improving EAF Furnace Efficiency
Technology Context in Vietnam
Several steel plants such as Pomina, Vina Kyoei, Thép Miền Nam, Dana, etc., use Electric Arc Furnace (EAF) technology to produce steel from scrap.
EAFs account for 25–30% of Vietnam’s steel industry and have the advantage of lower CO₂ emissions compared to blast furnaces.
However, operational efficiency remains suboptimal due to:
Inconsistent input materials (high impurity content)
Heat loss during charging and melting
Incomplete utilization of waste heat and generated gases
Applications in Vietnam
Pomina is implementing a waste heat recovery system and upgrading its arc control software.
Vina Kyoei is combining scrap and HBI (Hot Briquetted Iron) to improve steelmaking stability.
Thép Việt Đức is applying oxygen injection along with a supplementary induction furnace.
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS

## Slide 29
2.1 Optimizing Input Materials and Improving EAF Furnace Performance
Solution Group | Applicable content
Optimize input materials | Control of Si, Cu, S content in scrap, careful classification, use of reconstituted iron (HBI, DRI)
Pre-heating scrap (clean scrap steel) | Use hot gas or oxygen to heat before loading
Optimum oxygen and carbon injection | Support the reduction process, increase the melting speed
Furnace gas heat recovery | Used for scrap drying, or ORC power generation
Electrode optimization and power configuration | Reduce losses, control the arc effectively
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS

## Slide 30
Estimated Energy and Economic Efficiency
Assumption: A steel plant producing 500,000 tons of steel per year:
Reduced electricity consumption: from 650 → 580 kWh/ton of steel
Savings: 70 kWh × 500,000 = 35 million kWh/year
Average electricity price: 0.1 USD/kWh → Annual savings: ~3.5 million USD
Reduction in electrode consumption: ~15–20%
Increase in furnace productivity: ~10–15%
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS
2.1 Optimizing Input Materials and Improving EAF Furnace Performance

## Slide 31
Practical Applications in Vietnam
Hòa Phát Dung Quất has integrated casting and hot rolling to minimize gas consumption and improve overall plant efficiency.
Pomina is researching the use of billet heat to dry input materials and optimize reheating furnace energy.
Vina Kyoei has invested in a precision casting control system to reduce scrap.
Nhà máy thép Pomina
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS
2.2 Waste Heat Recovery and Optimization of Continuous Casting Process

## Slide 32
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS
2.2 Waste Heat Recovery and Optimization of Continuous Casting Process
Category | Technical Solution
Billet Waste Heat Recovery | Install systems to recover heat from billet radiation or use hot gas to dry input materials
Continuous Casting–Hot Rolling Integration (Hot Charging) | Transfer billets while still hot (800–1,000°C) directly to the rolling mill without reheating
Precise Control of Casting Speed & Cooling | Improve crystal structure, reduce cracking and defects
Optimization of Water Spraying and Pre-cooling | Reduce unnecessary heat loss and stabilize the solidification process

## Slide 33
Energy Savings Efficiency (Assuming 1 million tons of steel/year)
Heat saved by using hot charging (instead of reheating): ~80–100 m³ of gas/ton
Equivalent calorific value: ~400–500 MJ/ton of steel
Total energy saved: ~139,000 MWh/year
Fuel cost reduction: ~4–6 million USD/year
CO₂ emissions reduction: ~60,000–80,000 tCO₂/year
2. EEMs IN THE ELECTRIC ARC FURNACE (EAF) PROCESS
2.2 Waste Heat Recovery and Optimization of Continuous Casting Process

## Slide 34: 3. Energy Saving Opportunities in Auxiliary Systems
3.1 Compressed Air System
Item | Energy Saving Opportunity
Air Compressor | Replace with high-efficiency compressor using Variable Speed Drive (VSD) control
Air Leaks | Perform regular leak inspections, install leak detection devices, and repair promptly
Operating Pressure | Reduce system pressure (if appropriate) to lower electricity consumption
Operating Mode | Optimize compressor run time based on actual demand
Compressor Waste Heat | Recover heat from compressor exhaust air for other uses
Pressure Distribution | Optimize air pressure supply according to each production area

## Slide 35: 3. Energy Saving Opportunities in Auxiliary Systems
3. 2 Industrial Pump and Fan System
Item | Energy Saving Opportunity
Electric Motor | Replace IE1/IE2 motors with high-efficiency motors (IE3, IE4)
Load Control | Apply variable frequency drives (VFDs) to control pumps/fans instead of using mechanical throttling
Piping System | Reduce pressure losses by improving pipe design, cleaning fan blades and filters
Load Factor | Remove or optimize motors operating under 40% load
3.3 Recirculating Cooling System
Item | Energy Saving Opportunity
Cooling Tower | Optimize water flow and fan speed using variable speed drives (VSDs)
Circulation Water Pump | Install VSDs and optimize flow based on actual heat load
Operating Temperature | Increase inlet water temperature where possible to reduce power consumption

## Slide 36: 3. Energy Saving Opportunities in Auxiliary Systems
3.4 Lighting System
Item | Energy Saving Opportunity
Lamp Type | Replace fluorescent/halogen lamps with high-efficiency LED lights
Lighting Control | Install light sensors, motion detectors, and zone/time-based on-off control systems
3.5 Steam and Waste Heat Recovery System
Item | Energy Saving Opportunity
Pipe Insulation | Inspect and improve insulation to reduce heat loss
Condensate Recovery | Increase condensate return rate to save boiler fuel consumption
Waste Heat Recovery | Utilize excess heat from blast furnaces, coke ovens, and exhaust gases for drying materials, steam generation, or electricity production

## Slide 37
Installing energy metering systems, applying consumption benchmarks for each process, and using variable frequency drives (VFDs) to adjust motors can help reduce electricity consumption by 2.5-25%, depending on the equipment.
Software Interface(online access)
Software Interface(local/internal use)
4. OTHER OPPORTUNITIES
4.1 Effective energy management

## Slide 38
Data analysis – display & reporting
The collected data will be processed and analyzed into clear information for users regarding the energy consumption patterns of the facility.
The data is analyzed according to timeframes such as hourly, daily, weekly, monthly, etc. This helps identify peak consumption periods and areas with potential for energy efficiency.
The information is displayed visually through graphs and tables, making it easy for users to understand usage trends, costs, and other important data.
4. OTHER OPPORTUNITIES
4.1 Effective energy management

## Slide 39
Incident detection and warning
After being collected, the data is analyzed and examined by the system for any arising incidents. These incidents include
Overvoltage
Overcurrent and overload
Short circuit
….
Once detected, incidents will be recorded and summarized for the user. This helps users stay informed of any arising issues and determine appropriate solutions
4. OTHER OPPORTUNITIES
4.1 Effective energy management

## Slide 40
Dedicated feature – Management process according to ISO 50001 standard
The energy management standard is developed based on the guidelines of the Ministry of Industry and Trade.
Data is collected and analyzed in close accordance with the provided guidelines
Information is analyzed and displayed in a clear, simple, and visual chart format. This helps customers analyze and assess the effectiveness of energy use and the results of implemented management and upgrade solutions
4. OTHER OPPORTUNITIES
4.1 Effective energy management

## Slide 41
4. OTHER OPPORTUNITIES
4.1 Effective energy management
Feature | Practical Application in Production process | Key Benefits
Data analysis & reporting | Real-time dashboards for energy use patterns | 3%+ annual savings, clear usage insights
Incident detection | Alerts for voltage, overloads, short circuits | Less downtime, proactive response, cost avoidance
ISO 50001 conformity | Energy policies, targets, metrics, dashboards, reviews | ~5% energy cost reduction, savings compounding, improved maintenance & branding
Summary Table – Application vs Benefit

## Slide 42
4.2 Fuel conversion
Some factories have started replacing fuel oil (FO) with natural gas (NG), which helps reduce fuel costs (approximately 113,000 VND per ton of billets) and lowers emissions. In the future, the use of green hydrogen instead of coal in steelmaking could be a promising direction, although it is currently limited by costs and infrastructure.
Steel companies can integrate the use of solar or wind energy to reduce dependence on the national power grid, which is primarily based on fossil fuels. This not only saves long-term costs but also aligns with the trend of green steel production, meeting international requirements such as the EU's Carbon Border Adjustment Mechanism (CBAM).
4.3 Investment in renewable energy
4. OTHER OPPORTUNITIES
Example: PEB Steel & Vu Phong Energy Group
Partnership: Vu Phong Energy Group, an EPC and solar developer, installed rooftop solar systems for industrial clients in Vietnam—including a 1.04 MWp system for a steel manufacturer in Bắc Giang Province.
While not a primary steel producer, PEB Steel Buildings manufactures steel structures used by major brands like Nike, Samsung, Canon, etc. The solar project at their steel facility demonstrates how integrating solar can directly support steel industry operations.

## Slide 43: Example
Example: PEB Steel & Vu Phong Energy Group
Partnership: Vu Phong Energy Group, an EPC and solar developer, installed rooftop solar systems for industrial clients in Vietnam—including a 1.04 MWp system for a steel manufacturer in Bắc Giang Province.
While not a primary steel producer, PEB Steel Buildings manufactures steel structures used by major brands like Nike, Samsung, Canon, etc. The solar project at their steel facility demonstrates how integrating solar can directly support steel industry operations.
Benefit Area | Description
Energy Cost Savings | Rooftop solar reduces dependence on the grid—particularly fossil-fuel–based power—leading to long-term energy cost reductions.
Sustainability & CBAM Compliance | Using renewable energy lowers the indirect carbon footprint of steel products, helping meet EU’s Carbon Border Adjustment Mechanism (CBAM) requirements.
Grid Resilience | Partial off-grid solar supply helps stabilize energy access in the face of Vietnam’s often overburdened power infrastructure.
Corporate Brand Enhancement | Demonstrates leadership in sustainable manufacturing, boosting brand perception with global partners and clients.

## Slide 44
5. Tools for M&V the Effectiveness of EE Investments
Energy Baseline Analysis (Energy Baseline – EnB)
Objective: To serve as a basis for comparison before and after implementing energy-saving measures.
Method:
Use historical energy consumption data (typically 1–3 years).
Adjust for variations in production output, weather conditions, and operating load.
Supporting Tools:
Excel
ISO 50001 software
EnPI (Energy Performance Indicator) software by the U.S. Department of Energy (DOE)

## Slide 45
5. Tools for M&V the Effectiveness of EE Investments
Energy Performance Indicator Analysis (EnPI)
Objective: To continuously monitor energy consumption relative to product output.
Example Indicators:
kWh per ton of steel
GJ per ton of clinker
TOE per ton of product, etc.
Application:
Measure the effectiveness of investments after implementing energy-saving solutions (by reducing specific energy consumption).
Compare on a monthly/quarterly/annual basis.

## Slide 46
Advanced Financial Analysis (NPV, IRR, LCOE)
Simple Payback Period – SPB)
Formula:
Meaning: Determine the payback time, help make investment decisions.
Recommendation: Solutions with SPB < 3 years are usually preferred.
Tool | Description | Meaning
NPV (Net Present Value) | Net present value of savings benefits | NPV > 0 → Investment is recommended
IRR (Internal Rate of Return) | Internal rate of return of the project | IRR > cost of capital → Project is effective
LCOE (Levelized Cost of Energy) | Average cost of energy | Used to compare costs between different technologies
SPB =
Investment Cost​
Annual Cost Savings
5. Tools for M&V the Effectiveness of EE Investments

## Slide 47
Energy Monitoring and Management System (EMS – Energy Management System)
Objective: Monitor energy data in real time.
Functions:
Measure consumption of electricity, steam, compressed air, water, and fuel.
Compare with benchmarks (baseline, energy-saving targets).
Alert for anomalies (leaks, threshold exceedances).
Integrate with: ISO 50001, internal KPI reports, and GHG emission reduction plans.
Measurement & Verification (M&V – IPMVP)
Reference Standard: IPMVP – International Performance Measurement and Verification Protocol
Purpose: Ensure transparency in measuring energy savings.
Common M&V Methods:
Option A: Pre- and post-measurement with estimation
Option B: Direct, detailed measurement of parameters
Option C: Whole-facility analysis using energy bills
Option D: Energy modeling
5. Tools for M&V the Effectiveness of EE Investments

## Slide 48
Practical Application Suggestions
5. Tools for M&V the Effectiveness of EE Investments
Situation | Recommended Tools
Enterprise implementing ISO 50001 | EnPI + EMS + M&V
Reporting investment project outcomes | SPB, NPV, IRR
Monitoring monthly savings | KPI chart + energy baseline
Presenting to management | Visual dashboard (EMS) + short SPB

## Slide 49
5. CONCLUSION AND FUTURE TRENDS
The energy-saving opportunities in both blast furnaces and EAFs are significant, ranging from optimizing raw materials, waste heat recovery, PCI coal injection, to the application of hydrogen and digital technologies. Vietnamese steel plants are gradually implementing these solutions, but further policy support and investment in technology are needed to achieve maximum efficiency.
The future trend is to combine blast furnaces with hydrogen technology, electrification, and CO₂ gas recycling to move toward low-carbon steel production. EAF combined with green hydrogen, renewable electricity, and comprehensive heat recovery systems.
Hoa Phat and Formosa Ha Tinh have implemented several solutions such as:
  Recovering BFG gas for power generation.
  Injecting PCI coal to reduce coke consumption.
  Utilizing blast furnace slag as construction material.
  Challenges:
  High investment costs for advanced technologies.
  Lack of green hydrogen or affordable renewable energy sources.

## Slide 50: Q&A
Please share the actions in the EEMs activities of your business?

## Slide 51
THANK YOU